Example 1:

Determine the neutral axis depth if the following beam dimensions are known. Also calculate n1 from the equation dn = n1 d.

The neutral axis depth is given by:

From tables of the areas of round bars, As = 628 mm2

n1 is small because the steel is very little.

From the graph it can be seen that Mu/Mr = 0,64 which tells us that the concrete in the beam still has additional capacity.

Example 2:

A 220 mm wide beam is simply supported and spans 6 m. The beam carries the following loads.

Dead load = 	12 kN/m

Live load = 	18 kN/m

Concrete stress, fcu	= 30 MPa

Reinforcing stress, fy	= 450 MPa

wu	= 1,2 x DL + 1,6 x LL

= 1,2 x (12) + 1,6 x (18)

= 43,2 kN/m

Set the applied ultimate moment = the resistance moment

Solve for d

To this add cover and stirrup and round off to nearest 25 mm for practical reasons. Assume a 25 mm reinforcing bar. . Set h = 500 mm

Assume a bar diameter of 25 mm, stirrup = 12 mm and a cover of 25 mm. The new d = 500 - 25-12 - 25/2 = 450 mm.

From the graph we can read the percentage steel required:

% steel = 1,45%, i.e.,

| Bar size (mm) | Number of bars |
| --- | --- |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 |
| 6 | 28.3 | 56.5 | 84.8 | 113.1 | 141.4 | 169.6 | 197.9 | 226.2 | 254.5 | 282.7 |
| 8 | 50.3 | 100.5 | 150.8 | 201.1 | 251.3 | 301.6 | 351.9 | 402.1 | 452.4 | 502.7 |
| 10 | 78.5 | 157.1 | 235.6 | 314.2 | 392.7 | 471.2 | 549.8 | 628.3 | 706.9 | 785.4 |
| 12 | 113.1 | 226.2 | 339.3 | 452.4 | 565.5 | 678.6 | 791.7 | 904.8 | 1017.9 | 1131.0 |
| 16 | 201.1 | 402.1 | 603.2 | 804.2 | 1005.3 | 1206.4 | 1407.4 | 1608.5 | 1809.6 | 2010.6 |
| 20 | 314.2 | 628.3 | 942.5 | 1256.6 | 1570.8 | 1885.0 | 2199.1 | 2513.3 | 2827.4 | 3141.6 |
| 25 | 490.9 | 981.7 | 1472.6 | 1963.5 | 2454.4 | 2945.2 | 3436.1 | 3927.0 | 4417.9 | 4908.7 |
| 32 | 804.2 | 1608.5 | 2412.7 | 3217.0 | 4021.2 | 4825.5 | 5629.7 | 6434.0 | 7238.2 | 8042.5 |

Steel required = 3 ( 25 (1470)

Example 3:

A slab is placed over a double garage with dimensions 6 m x 10 m. The space above is to be used as a studio with office loading of 2,5 kN/m2. The floor finish has a weight of 1,0 kN/m2. Determine the slab thickness, the weight on the slab and the reinforcing. Assume that the slab is simply supported on all 4 sides. Use a 25 MPa concrete, high tensile reinforcing and 20 mm cover.

Slab thickness	 = smaller span / 28	= 6000 / 28	= 214 mm

Use standard brick plus mortar layer dimensions of 85 mm, therefore use 3 x 85 = 225 mm.

Self weight of slab	= 0,225 x 24 kN/m3	= 5,4 kN/m2

Floor finish					= 1,0 kN/m2

Total permanent or dead load			= 6,4 kN/m2

Live load					= 2,5 kN/m2

Factored load wu	= 1,2 x DL + 1,6 x LL	= 1,2 x 6,4 + 1,6 x 2,5

= 11,68 kN/m2

Assume a 1 m wide strip of the slab.

The uniformly distributed load on the 1 m wide slab is then 11,68 kN/m

Ratio of longer span to shorter span =

| Ly/Lx | 1,0 | 1,1 | 1,2 | 1,3 | 1,4 | 1,5 | 1,75 | 2,0 | 2,5 | 3,0 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| X | 0,062 | 0,074 | 0,084 | 0,093 | 0,099 | 0,104 | 0,133 | 0,118 | 0,122 | 0,124 |
| Y | 0,062 | 0,061 | 0,059 | 0,055 | 0,051 | 0,046 | 0,037 | 0,029 | 0,020 | 0,014 |

Table for moments in the two directions:

SX	= 0,110

SY	= 0,040

Assume 16 mm diameter bars. Depth to the centre of the reinforcing bars = 255 – 20 – 16/2 = 227 mm

From the graph we can determine the percentage steel:

% ASX	= about 0,24%

% ASY	= about 0,12%

Use a minimum of 0,12% for the steel in the Y-direction.

ASX = 0,24 x 1000 x 227 /100	= 545 mm2

ASY = 0,12 x 1000 x 211 /100	= 254 mm2

| Spacing (mm) | Bar Diameter |
| --- | --- |
|  | 8 | 10 | 12 | 16 | 20 | 25 | 32 |
| 100 | 503 | 785 | 1131 | 2011 | 3142 | 4909 | 8042 |
| 125 | 402 | 628 | 905 | 1608 | 2513 | 3927 | 6434 |
| 150 | 335 | 524 | 754 | 1340 | 2094 | 3272 | 5362 |
| 175 | 287 | 449 | 646 | 1149 | 1795 | 2805 | 4596 |
| 200 | 251 | 393 | 565 | 1005 | 1571 | 2454 | 4021 |
| 225 | 223 | 349 | 503 | 894 | 1396 | 2182 | 3574 |
| 250 | 201 | 314 | 452 | 804 | 1257 | 1963 | 3217 |
| 275 | 183 | 286 | 411 | 731 | 1142 | 1785 | 2925 |
| 300 | 168 | 262 | 377 | 670 | 1047 | 1636 | 2681 |

Cross-section area of reinforcing bars spaced at various intervals.

Steel in the shorter direction use  12 mm at 200 mm spacing with an area of 565 mm2.

Steel in the shorter direction use  10 mm at 250 mm spacing with an area of 314 mm2.

It is always a good idea to supply torsional steel in the corners of slabs as these will tend to crack if not reinforced properly. It should consist of top and bottom steel each with layers of bars placed parallel to the sides of the slab and extending a distance of one fifth of the span. The area should be three quarters of the maximum steel in the centre.

75% of 545 = 409 mm2. Use Y10 @200 with an area of 393 mm2.

Use minimum steel in Y-direction.

Typical layout for a simply supported flat slab.

Doubly reinforced beams.

If the ultimate moment is greater than the maximum resistance moment of the beam, i.e., Mu > Mrc (Concrete) Then additional steel may be provided on the compression side of the member. The strain at which this steel functions is limited by the strain at which the concrete functions at ultimate strength. The resistance of the steel is then limited by the strain.

Section with compression and tension steel.

The total resistance moment of the section, Mr = Mrc(max) + M’rs

Compression steel resistance moment

Concrete resistance moment

It is now possible to determine the area of the compression steel.

For horizontal equilibrium:

Compression force 			= 	Tension force

=

It then follows that the tensile steel area:

The total moment of resistance:

Example 4:

A 220 x 500 x 25 MPa beam has an applied ultimate moment of 200 kN.m. Determine the required reinforcing in the member.

The ultimate maximum resistance moment of the concrete. Estimate the bar size to be 2 layers of 25 mm with a 25 mm between. The cover is 25 mm. The depth d = 500 –25 (cover) – 12 (stirrup) – 25 (bar size) – 25/2 (half distance between bars) = 425 mm

. The beam requires compression steel.

Assume 25 mm bars in compression with 25 mm cover to the steel. The distance to the centre of the compression steel, d’, = 25 + 12 (stirrup) + 25/2 = 50 mm

(2  20 mm bars with area of 628 mm2)

Determine the tension reinforcement:

Use 2  25 (982 mm2)+ 2  20 (628 mm2)

T and L – beams

T and L – beams are found when concrete is saved by using hollow block floors, waffle (coffer) slabs, slabs with ribs or trough slabs.

Thickness of slabs over hollow blocks and between ribs.

The following may be used as a rough estimate:

Hollow block floors: 40 mm or one-tenth of the distance between ribs, whichever is greater.

Ribbed floors without permanent blocks: 50 mm or one-tenth of the distance between ribs, whichever is greater.

Rib-width should not be less than 65 mm and spaced at no more than 1500 mm.

Effective width of compression flange.

The effective width of the compression flange depends on the spacing of the ribs and the span and is not necessarily the distance between the ribs. The effectiveness is determined by the shear flow.

T-beam: The lesser of (a) the width of the web bw plus one-fifth of the distance between positions of zero moment or (b) the spacing of the ribs.

L-beam: The lesser of (a) the width of the web bw plus one-tenth of the distance between positions of zero moment or (b) the spacing of the ribs.

Design Procedure:

Two cases are possible:

Firstly the neutral axis may lie in the slab.

Assume that the neutral axis is in the flange:

Calculate the lever arm, z = a1 d.

With the value of z known it is possible to calculate dn using the equation:

If dn is less than hf calculate the tension steel as usual:

Secondly the neutral axis may lie in the web.

This will happen if dn is greater than hf.

The resistance moment of the concrete is given by:

and this must be greater than the applied ultimate moment, Mu. If Mu is greater than the resistance moment of the concrete, compression steel must be added.

If Mrc > than Mu:

Example 5:

A hollow block floor spans 8 m. The blocks are 500 x 375 mm and weigh 1 kN/m. The floor finish has a weight of 0,9 kN/m2. A live load of 2,5 kN/m2 is applied to the floor. Determine the required reinforcing to the beam. Concrete 25 MPa after 28 days.

Preliminary size

In a 650 mm wide strip:

Dead load hollow block:								= 1,00 kN/m

Concrete	Area x unit weight	= (0,65 x 0,075 + 0,375 x 0,15) x 24	= 2,52 kN/m

Floor finish	width x unit weight	= 0,65 x 0,9				= 0,586 kN/m

## Total dead load								= 4,106 kN/m

## Live load	width x unit load	= 0,65 x 2,5				= 1,625 kN/m

## Factored load	1,2 x DL + 1,6 x LL	= 1,2 x 4,106 + 1,6 x 1,625		= 7, 53 kN/m

Ultimate moment

Cover = 25 mm. Assume 25 mm high tensile bars.

d = 450 – 25 –10 (stirrups)– 25/2 = 402,5 mm, lets call it 400 mm

Calculate the lever arm

Maximum value = 0,95

z 	= a1. d		0,95 . 400	= 380 mm

The neutral axis falls within the flange.

Use 2 x  16 mm bars with an area of 402 mm2.

Cover = 25 mm. Assume 16 mm high tensile bars.

d = 450 – 25 –10 (stirrups)– 16/2 = 407 mm

z 	= a1. d		0,95 . 407	= 386 mm

Alternative design method:

Use the design table.

% steel required = 0,15%

As = 0,15 x 650 x 407/100	= 397 mm2

Reinforced Concrete Columns

Columns carry the loads from roofs, floors and beams to the foundations (footings) in compression and bending. Bending moments may be present if frame action is used to carry wind loads and beam loads. In this course only axial loads will be taken into account.

Failure of columns.

Columns may fail in one of or a combination of the following failure mechanisms.

# Reinforcing of Concrete Columns

Reinforcing increases the capacity of the column to resist both axial forces and bending moments.

# Column Alignment and Spacing

Reducing the spacing of columns will lead to reduced slab and beam thicknesses. Too many columns close together will limit the floor space and the structure will appear to be “busy”. For planning, a minimum column spacing of 4 m in the one direction and 5 m in the other direction is recommended with an ideal spacing of between 6 m and 7,5 m in both directions. In some situations such as the basement of high buildings, a column spacing of 10 m may be both functional and economical.

Beam and slab construction, coffer slabs and post-tensioned slabs make bigger column spacing possible, i.e., 10 m to 12 m.

# Column Shapes and Economy

It is possible to cast concrete columns in almost any cross-sectional shape. Unusual shapes require made-for-purpose shuttering, which will be expensive. Symmetrical shapes such as rectangles and round are the preferred shapes.

It is uneconomical to change the column dimensions on each floor of multi-storey buildings just to reflect the change in the load. The dimensions are usually kept constant and the amount of reinforcing is varied between 1% and 6%.

Shutter suppliers generally keep standard shutter sizes. Deviation from standard sizes can increase the cost of the building. The following sizes should be considered:

Typical column boxes.

Cross-sectional dimensions: 225 mm to 900 mm in increments of 75 mm.

Column height: up to 3,6 m.

Vertical Loads Carried by Columns.

Column load varies not only in plan but also in height.

Practical Estimated Column Sizes for Multi-Storey Buildings.

Keep minimum parking bay size in mind if there is basement or other parking:

Typical minimum parking bay size.

The following table may be used to estimate the size of concrete columns in multi-storey office or apartment buildings.

| Column spacing (mxm ) | For the bottom level: Estimated column sizes (mm x mm) |
| --- | --- |
|  | Number of storeys – offices or apartments |
|  | 2 | 4 | 6 | 8 | 10 | 12 |
| 5 x 5 |  |  |  | 400 x 400 |  |  |
| 6 x 6 |  |  | 400 x 400 | 500 x 500 |  |  |
| 7 x 7 | 300 x 300 | 375 x 375 | 450 x 450 | 600 x 600 |  |  |

Design of Columns for Adequate Axial Strength.

Short stocky columns usually fail in crushing of the material whereas long slender columns may buckle. To avoid buckling ensure that the slenderness is not too large>

Stocky columns

Slender columns

le is the effective length

bmin is smaller cross-sectional dimension.

Slender columns require special design considerations, this course will be restricted to stocky columns.

Axial Resistance of Stocky Columns.

The axial resistance:

fcu	= characteristic concrete cube strength

fy	= yield stress of the reinforcing

Ac	= cross-sectional area of the concrete

Asc	= cross-sectional area of the reinforcing steel.

The resistance, Cr must be greater than the ultimate load, Cu.

Cu is usually based on 1,2 x DL + 1,6 x LL.

For initial design purposes it is recommended that Asc < 2% of the concrete cross-sectional area.

Asc < 0,02 Ag where Ag = b x b.

Because Ag = Ac + Asc

It follows that Ac = 0,98 Ag

Then

If Cu, fcu and fy are known it is easy to calculate Ag = b2

Example 1:

A reinforced concrete column is 5 m long and carries the service loads of:

Dead load = 600 kN

Live Load = 400 kN.

Assume fcu = 35 MPa and fy = 450 MPa.

The column is fixed top and bottom. Determine a suitable column size and reinforcing.

Ensure that the column is stocky, i.e., Le/b < 12.

Le = 0,7 x L = 0,7 x 5000 = 3500 mm.

Use a 300 x 300 mm column.

Cu = 1,2 x DL + 1,6 x Imposed Load	= 1,2 x 600 + 1,6 x 400	= 1360 kN

1102500 – 12,25 Asc + 270 Asc > 1360 x 103

Asc > 999 mm2

Use 4 Y20 with an area of 1256 mm2.

Example 2:

Determine preliminary sizes of the columns of the 5 storey office block. Assume:

2,5 kN/m2 for live load

0,5 kN/m2 for partition loads

Concrete strength = 35 MPa

Steel yield strength = 450 MPa

Estimate the floor thickness =

Use a thickness of 250 mm

Area carried by column = 8 x 6 m2 / floor = 48 m2

Total area carried by column 	= 48 x 5 floors (first floor to roof inclusive)

= 240 m2

Dead or permanent load, DL:	Slab	= 0,25 x 24	= 6,0 kN/m2

Partitions		= 0,5 kN/m2

Total			= 6,5 kN/m2

Imposed load (live load), IL				= 2,5 kN/m2

wu = 1,2 x DL + 1,6 x IL		= 1,2 x 6,5 + 1,6 x 2,5	= 11,8 kN/m2

Total load on column		= Area x wu

= 240 x 11,8 		= 2832 kN

Assume that we are going to use 2% steel

Ag = Aconcrete + Asc

Ag > 162711 mm2

b2 > 162711 mm2

b > 403 mm

Use a 400 x 400 mm cross-section.

1969 x 103 – 12,25 Asc + 270 Asc > 2832 x 103

Asc > 3384 mm2

Use 8 Y 25 reinforcing rods.

## Concrete Footings

The primary purpose of a footing is to ensure that the axial loads from columns and walls are safely transferred to the ground and that the stress on the ground does not cause undue displacement. To ensure that the displacement is not too large, the stress as a result of service loading may not exceed the allowable. For the design of the reinforcing in the footing, ultimate loads must be used.

The following structural aspects must be investigated in the design of the footing.

- The plan surface area must be large enough to safely transfer the service loads

- The footing must have sufficient resistance moment to resist the ultimate moment induced by the soil pressure

- The footing must have sufficient shear resistance to resist the ultimate shear induced by the soil pressure.

- The punching resistance must be large enough.

Foundations should be thick enough that punching shear and normal shear are not a problem.

Example 3:

Design a reinforced footing for the following:

- 300 x 300 mm column

- service load	Dead load = 600 kN, Imposed load = 400 kN

- Allowable soil pressure	= 300 kN/m2 (kPa)

- fcu 	= 25 MPa,

- fy	= 250 MPa

Solution:

Area of footing

Use a square footing,

Set b = 1850 mm

Assume a preliminary thickness of :

Use a thickness of 450 mm.

Design the footing for bending moment; we must therefore use ultimate forces and moments.

Ultimate load = 1,2 x DL + 1,6 x IL	= 1,2 x 600 + 1,6 x 400	= 1360 kN

Pressure under the footing

Calculate the moment at the interface between the column and the footing:

Ensure that Mcr > Mu otherwise compression steel will be required.

Cover to reinforcing = 75 mm for foundations.

d = 450 – 75 –25/2 = 362,5 mm, use 360 mm (We assume 25 mm bars hence 25/2 subtracted)

z = a1.d

Use R25 @ 300 mm (1636 mm2) in both directions.

# Test for Shear

Vu = 0,235 x 1,850 x 397 = 172,6 kN

If % steel =

With fcu = 25 MPa and % steel = 0,246%, the design table gives a vcr = 0,38 MPa which is greater than the induced shear stress.

# Punching Shear

Punching circumference 	= 4 x 300 +  x D

= 4 x 300 +  x 3 h

= 4 x 300 +  x 3 x 450

= 5441 mm

Hatched area will tend to stay behind as column tries to punch through.

Hatched area 	= 18502 – (300x300 + 4x300x675 + x6752)

= 1,091 x 106 mm2

= 1,091 m2

Vpunching		= 1,091 x 397	= 433,13 kN

Punching stress

REINFORCED CONCRETE – ADDITIONAL PROBLEMS

Question1:

Determine the neutral axis depth as well as the resistance moment of the concrete beam with the following cross-sectional dimensions. Concrete is a grade 30 MPa, i.e., fcu = 30 MPa, bars are high tensile with a yield stress of 450 MPa. (Answer dn = 146 mm, M = 150,1 kN.m)

Question 2:

A simply supported 250 mm wide beam, spans 8 m and carries the following serviceability (unfactored) loads. Determine the required height, h, and the tensile steel. (One possible set of answers: h = 575 mm, As = 1512, i.e., 2 x 25 mm + 2 x 20 mm bars)

DL = 10 kN/m

LL = 12 kN/m

Concrete grade 		= 25 MPa

Reinforcing stress 	= 450 MPa

Question 3:

You are asked to design a simply supported concrete slab over a garage with dimensions 4,5 m x 6 m. The floor carries a live load of 1,5 kN/m2 and an additional dead load from the floor finish of 1,2 kN/m2. Use a grade 25 MPa concrete and high tensile steel, fy = 450 MPa with the cover to the steel = 20 mm. Determine the thickness of the slab and the reinforcing in both directions. (Possible answers: Thickness = 170 mm, wu = 8,736 kN/m2, Mux = 17,5 kN.m, Muy = 9,73 kN.m, Asx = 331 mm2/m, Asy = 198 mm2/m)

Question 4:

A 250 x 600 mm concrete beam with a concrete strength of 25 MPa has an ultimate applied moment of 330 kN.m. Yield stress of bars = 450 MPa, cover to bars = 25 mm. Determine the tension and compression steel. (Answers: A’s = 369 mm2, As = 2018 mm2)